|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Date of Testing** | | 29-08-2022 | | **COA No:** | | | | COA044 | | | |
| **Material Name** | | SS | | **Batch/Lot No. (If Available)** | | | | Boo5678 | | | |
| **Material Quantity** | | 47 | | **Any reference** | | | |  | | | |
| **Manufacturing date** | | 23-08-2022 | | **Expiry date** | | | | 31-08-2022 | | | |
| **Sr. No.** | **Testing Parameter** | **Testing Method** | **Acceptance Criteria** | | **Sampling Method** | **Observations** | | | | | **Remarks** |
| **1** | **2** | | **3** | **4** |
|  | Thickness | Vernier caliper | 10.0±0.1 | | Refer SOP for inspection | 10.03 | 9.97 | | 9.9 | 10.08 |  |
|  | Width | Vernier caliper | 5.0±0.1 | | 4.98 | 4.99 | | 4.99 | 5.0 |  |
|  | Length | Vernier caliper | 30.0±1.0 | | 29.48 | 30.48 | | 30.31 | 29.65 |  |
|  | Hole size | Vernier caliper | 2.0±0.05 | | 1.96 | 1.96 | | 1.98 | 1.99 |  |
|  | Shape | Visual | Similar | | Similar | Similar | | Similar | Similar |  |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| √ | **Approved** | **Comments/Instructions:** | **Inspected By** | Sumit |
| × | **Rejected** |  |
| **Verified and Approved By** | Rajiv |